COMMON ANODE TYPE PIN PHOTO DIODE.

HIGH SPEED SENSITIVITY.

●DIE SIZE                   2.27㎜ × 2.27㎜

●DIE THICKNESS400         300 ± 20um

●METALLIZATION

TOP         Al

BOTTOM    Ag

●PASSIVATION               Silicon oxide

●BONDING PAD SIZE

CATHODE       140um × 140um

ANODE (BOTTOM)

●ACTIVE AREA              1.34mm ×1.34mm

●ABSOLUTE MAXIMUM RATINGS ( Ta = 25℃ )

| Parameter | Symbol | Maximun rating | Unit |
| --- | --- | --- | --- |
| Reverse Breakdown Voltage | BVR | 30 | V |
| Junction Temperature | TJ | 150 | ℃ |

●ELECTRICAL / OPTICAL CHARACTERISTICS ( Ta = 25℃ )

| Parameter | Symbol | Condition | Min | Typ | Max | Unit |
| --- | --- | --- | --- | --- | --- | --- |
| Forward Voltage | VF | IF=10mA， | 0.5 |  | 1.3 | V |
| Reverse Breakdown Voltage | BVR | IR=10uA | 30 |  |  | V |
| Dark Current | ID | VR=10V |  | 1.6 | 10 | nA |
| Spectrum Sensitivity | λ |  | 430～1100 |  |  | nm |
| Peak Sensing Wavelength | λP |  |  | 940 |  | nm |

Note(1):Parallel light of 1,000Lux illumination is applied by a Tungsten lamp of 2856k.

2270

140

2270

140

地址： 深圳市宝安44区创业一路富源中心B703      邮编：518010

电话：0755-29129090